## Slide 1
VNA
Cable
Port I
Microstrip
PCB cell
Sample
Cable
Port II
Microstrip
PCB cell
Stage I:
SOLT/TOSM
SOLT/TOSM – standard 2-port VNA calibration procedure with the coaxial terminations (R&S mechanical cal kit)
Stage II:
Deembedding
Stage II:
Deembedding
Stage III:
Delay Time Compensation
Straight PCB cell
Dogbone PCB cell

## Slide 2
VNA
Long antenna cable
Sample
Short cable before the switching box
Port II
Long antenna cable
Short cable before the switching box
Port I
Stage I:
SOLT/TOSM
Antenna and free space
Stage II:
Deembedding
Stage II:
Deembedding
Stage III:
Response&Isolation
TRL
Stage III:
Response&Isolation
TRL
SP4T RF switch inside the antenna pillars
with SOL/OSM coaxial terminations
SP6T RF switches at the switching box with SOLT/TOSM coaxial terminations

## Slide 3
Choose parallel lines in the phase dispersion
The frequency range may include the phase jumps but they must be “clear”, not as in this graph on the right
That is why we will choose only the second line after the multiple jumps on the left and before the jumps on the right
Even for this part (without jumps), we will select a narrower frequency range
Such multiple jumps must be excluded from consideration
Frequency range that will be used for calculation of the delay time
Such single “shift” is also undesirable

## Slide 4
Although the two phase dispersion lines before and after the jump do not look perfectly parallel, we could try to combine them into an unwrapped phase.
Clear jump
Frequency range that will be used for calculation of the delay time

## Slide 5
Unwrapping

## Slide 6
Z, 
Frequency, Hz
Impedance dispersion measured in a ferromagnetic wire
Z
Spikes due to numerical uncertainties caused by the 2-port deembedding
The delay time has been tuned for this frequency range